## Slide 1
THE MONOLITHIC 3D-IC: Logic + eDRAM on top

## Slide 2: How get single crystal silicon layers at less than 400oC (Required for stacking atop copper/low k)

## Slide 3: How are all SOI wafers manufactured today?
Activated n Si
Oxide
Oxide
H
Top layer
Bottom layer
Oxide
Hydrogen implant
of top layer
Flip top layer and
bond to bottom layer
Oxide
H
Cleave using 400oC
anneal or sideways
mechanical force. CMP.
Oxide
Activated n Si
Activated n Si
Activated n Si
Silicon
Silicon
Silicon
Using Ion-Cut (a.k.a. Smart-Cut) technology
Top layer

## Slide 4: Ion-cut (a.k.a Smart-CutTM)  Can also give stacked defect-free single crystal Si layers atop Cu/low k
Activated n Si
Oxide
Oxide
H
Top layer
Bottom layer
Oxide
Hydrogen implant
of top layer
Flip top layer and
bond to bottom layer
Oxide
H
Cleave using 400oC
anneal or sideways
mechanical force. CMP.
Oxide
Activated n Si
Activated n Si
Activated n Si

## Slide 5: Ion-cut vs. other types of stacked Si
 | Poly Si with RTA | Ion-cut Si
Defect density | High | Perfect single crystal Si.
Mobility | 100cm2/Vs | 650cm2/Vs
Variability | High | Low
Sub-threshold slope and Leakage | High | Low
Temperature stacked bottom layer exposed to typically | 700-800oC for crystallization | <400oC
Cost | Low | See next slide

## Slide 6: Ion-cut is great, but will it be affordable? Aren’t ion-cut SOI wafers much costlier than bulk Si today?
Today: Single supplier  SOITEC. Owns basic patent on ion-cut.
Our industry sources + calculations  $50 ion-cut cost per $1500-$5000 wafer in a free market scenario (ion cut = implant, bond, anneal).
Free market scenario  After 2012 when SOITEC’s basic patent expires
SiGen and Twin Creeks Technologies using ion-cut for solar
Contents:
Hydrogen implant
Cleave with anneal
SOITEC basic patent expires 2012!!!

## Slide 7: Monolithic 3D Logic Shorter wires. So, gates driving wires are smaller.

## Slide 8: TSV vs. Monolithic 3D 10,000x higher connectivity
TSV size typically >>1um: Limited by alignment accuracy, silicon thickness
Monolithic offers 10,000x higher connectivity than TSV
Processed Top Wafer
Processed Bottom Wafer
Align and bond
 | TSV | Monolithic
Layer Thickness | ~50m | ~50nm
Via Diameter | ~5m | ~50nm
Via Pitch | ~10m | ~100nm
Wafer (Die) to Wafer Alignment | ~1m | ~1nm
TSV

## Slide 9: Industry Roadmap for 3D with TSV Technology
TSV size ~ 1um, on-chip wire size ~ 20nm  50x diameter ratio, 2500x area ratio!!!
Cannot move many wires to the 3rd dimension
ITRS
2010

## Slide 10: Monolithic 3D: The Other Option Needs Sub-400oC Transistors
Junction Activation: Key barrier to getting sub-400oC transistors
Transistor part | Process | Temperature
Crystalline Si for 3D layer | Bonding, layer-transfer | Sub-400oC
Gate oxide | ALD high k | Sub-400oC
Metal gate | ALD | Sub-400oC
Junctions | Implant, RTA for activation | >400oC
In next few slides, will show 3 solutions to this problem…

## Slide 11: One path to solving the dopant activation problem: Recessed Channel Transistors with Activation before Layer Transfer
p- Si wafer
Idea 1: Do high temp. steps (eg. Activate) before layer transfer
Oxide
H
Idea 2: Use low-T processes like etch and deposition to define recessed channel transistors, the standard transistor type used in all DRAMs today. STI not shown for simplicity.
Note:
All steps after Next Layer is attached to Previous Layer are @ < 400oC!
n+
p
p- Si wafer
p
n+
n+ Si
p Si
n+
n+
p
p
Idea 3: Silicon layer very thin (<100nm), so transparent, can align perfectly to features on bottom wafer
Layer transfer

## Slide 12: Recessed channel transistors used in manufacturing today  easier adoption
n+
n+
p
GATE
n+
n+
p
GATE
GATE
V-groove recessed channel transistor: Used in the TFT industry today
RCAT recessed channel transistor:
Used in DRAM production
@ 90nm, 60nm, 50nm nodes
Longer channel length  low leakage, at same footprint
J. Kim, et al. Samsung, VLSI 2003
ITRS

## Slide 13: RCATs vs. Planar Transistors: Experimental data from Samsung 88nm devices
From [J. Y. Kim, et al. (Samsung), VLSI Symposium, 2003]
RCATs  Less DIBL i.e. short-channel effects
RCATs  Less junction leakage

## Slide 14: RCATs vs. Planar Transistors (contd.): Experimental data from Samsung 88nm devices
From [J. Y. Kim, et al. (Samsung), VLSI Symposium, 2003]
RCATs  Higher I/P capacitance
RCATs  Similar drive current to standard MOSFETs  Mobility improvement (lower doping) compensates for longer Leff

## Slide 15
MonolithIC 3D Inc. Patents Pending
15
Step 1 - Implant and activate unpatterned N+ and P- layer regions in standard donor wafer at high temp. (~900oC) before layer transfer. Oxidize (or CVD oxide) top surface.
Step 1. Donor Layer Processing
Step 2 - Implant H+ to form cleave plane for the ion cut
N+
P-
P-
SiO2 Oxide layer (~100nm) for oxide -to-oxide bonding with device wafer.
N+
P-
P-
H+ Implant Cleave Line in N+ or below
Notes: 15
15

## Slide 16
MonolithIC 3D Inc. Patents Pending
16
Step 3 - Bond and Cleave: Flip Donor Wafer and Bond to Processed Device Wafer
Cleave along
H+ implant line using 400oC anneal or sideways mechanical force.
Polish with CMP.
-
N+
P-
Silicon
SiO2 bond layers on base and donor wafers (alignment not an issue with blanket wafers)
<200nm
Processed Base IC
Notes: 16
16

## Slide 17
MonolithIC 3D Inc. Patents Pending
17
Step 4 - Etch and Form Isolation and RCAT Gate
+N
P-
Gate
Oxide
Isolation
Litho patterning with features aligned to bottom layer
Etch shallow trench isolation (STI) and gate structures
Deposit SiO2 in STI
Grow gate with ALD, etc. at low temp
(<350º C oxide or high-K metal gate)
Ox
Ox
Gate
Advantage: Thinned donor wafer is transparent to litho, enabling direct alignment to device wafer alignment marks: no indirect alignment.
Processed Base IC
Notes: 17
17

## Slide 18
MonolithIC 3D Inc. Patents Pending
18
Step 5 – Etch Contacts/Vias to Contact the RCAT
+N
P-
Processed Base IC
Complete transistors, interconnect wires on ‘donor’ wafer layers
Etch and fill connecting contacts and vias from top layer aligned to bottom layer
Processed Base IC
Notes: 18
18

## Slide 19: Compare 2D and 3D-IC versions of the same logic core with IntSim
MonolithIC 3D Inc. Patents Pending
19
22nm node 600MHz logic core | 2D-IC | 3D-IC 2 Device Layers | Comments
Metal Levels | 10 | 10 | 
Average Wire Length | 6um | 3.1um | 
Av. Gate Size | 6 W/L | 3 W/L | Since less wire cap. to drive
Die Size (active silicon area) | 50mm2 | 24mm2 | 3D-IC  Shorter wires  smaller gates  lower die area  wires even shorter 3D-IC footprint = 12mm2
Power | Logic = 0.21W | Logic = 0.1W | Due to smaller Gate Size
 | Reps. = 0.17W | Reps. = 0.04W | Due to shorter wires
 | Wires = 0.87W | Wires = 0.44W | Due to shorter wires
 | Clock = 0.33W | Clock = 0.19W | Due to less wire cap. to drive
 | Total = 1.6W | Total = 0.8W | 

## Slide 20: SoC Device Architecture
Pull out the memory to the second layer
  50% of SoC is embedded memory, 50% of the logic area is due to gate sizing buffers and repeaters.
    => Base layer 25%, just the logic
    => 2nd layer eDRAM with stack capacitor
  25% of the area of eDRAM (1T) needs to replace 50% of the equivalent SRAM
    1T vs. ½ of 6T ~ 1:3, could be used for:
      Use older node for the eDRAM, with optional additional port for independent refresh
    Additional advantage for dedicated layer of eDRAM
      Optimized process
      Only 3 metal layers, no die area wasted on loigic 10 metal layers
      Repetitive memory structure – easy for litho and fab

## Slide 21: 2D SoC to Monolithic 3D (eDRAM on top of Logic)
2D SoC
3D SoC
7mm
7mm
14mm
14mm
Logic + Memory
Logic
Memory
Footprint = 196mm2
Footprint = 49mm2

## Slide 22: Monolithic 3D SoC Side View
Base wafer with Logic circuits
RCAT transistors
(eDRAM + Decoders)
Stack Capacitors (for eDRAM)
Logic circuits

## Slide 23: eDRAM
Use RCAT for bit cell and decoders
Bit Line
WL
Vdd
Vdd
Bit Line
WL
WL-Refresh
eDRAM with independent port for refresh

## Slide 24: eDRAM vs SRAM on top
Smaller area and shorter lines should result in competitive performance
Independent port for refresh should allow reduced voltage and therefore comparable power

## Slide 25: Summary
First use of MonolithIC 3D technology for SoC could be pulling out the embedded memory to a 2nd layer
2nd Layer embedded memory could use RCAT + Stack Capacitor
EDA may need to be adjusted but existing EDA could be used by modifying the memory library and other software shortcuts
Estimated benefits:
  ~1/3 Device cost (first layer size is ~1/4 and second layer is low cost using older process node, repetitive layout, and only 3 metal layers)
  ½ power
  Comparable or better performance