## Slide 1
The Short, Medium and Long-Term Path to the 3D Ecosystem
Panel Discussion at EDPS
A Monolithic 3D-IC Perspective
Deepak C. Sekar

## Slide 2: Two Types of 3D Technology
3D-TSV
Transistors made on separate wafer @ high temperature, then thin + align + bond
TSV pitch > 1um*
Monolithic 3D
Transistors made monolithically atop wiring (@ sub-400oC for logic)
TSV pitch ~ 50-100nm
10um-
50um
100 nm
* [Reference: P. Franzon: Tutorial at IEEE 3D-IC Conference 2011]

## Slide 3: A Process Flow for Monolithic 3D: Recessed Channel Transistors with Activation before Layer Transfer
[D. C. Sekar, Z.Or-Bach, “Monolithic 3D-ICs with Single Crystal Silicon Layers”, Proc. IEEE 3DIC Conference 2011 (Invited)]
p- Si wafer
Activate dopants
Oxide
H
n+
p
p- Si wafer
p
n+
Layer transfer un-patterned film. No alignment issues.
Well-aligned sub-400C RCATs Si thickness < 100nm
Min. feature size TSVs since low Si thickness, no misalignment issues
n+
p
Steps atop Cu/low k < 400oC
RCATs used in production DRAM since the 90nm node
 Adoption easier
n+
p
n+
p

## Slide 4: SRAM-Logic Stacking
SRAM requirements different from logic today. Different number of metal levels, Vt, Leff...
Ultra-dense vertical connectivity needed, esp. for small size SRAMs within a logic core  good fit for Monolithic 3D
Logic Circuits
12 metal levels
Optimized SRAM
5 metal levels
can save process cost, and improve performance.
Ultra-dense connectivity
Ref.: [D. Sekar, PhD Thesis, Georgia Tech]
EDA need: Tools to partition designs and stack the SRAM

## Slide 5: Logic-Logic Stacking with High TSV Density
Modify existing 2D tools slightly
TSVs in whitespace or modify existing layout slightly for TSVs to stacked layer
OK for today’s 5um TSVs (low density)
Today
“Pseudo-3D” EDA Tools
Needed for Monolithic 3D
“Native-3D” EDA Tools
3D routing, placement, floorplanning tools that work for TSVs close to min. feature size
Support for both block-level and gate-level partitioning
Logic
DRAM

## Slide 6: Power Distribution Network Design
Thermal-Aware Place-and-Route
Most logic gates have VDD and GND contacts Low (thermal) resistance power grids  low temp. drop between heat sink and stacked logic gate
Promising simulation results
VDD
GND
EDA need: Integrate power distribution design with (thermal-aware) place-and-route for monolithic 3D
=
Good heat removal
for monolithic 3D
Ref.: [D. Sekar, Z. Or-Bach, US Patent Application #13/041,405]

## Slide 7: How will monolithic 3D technology tackle this familiar problem?
Suggestion to the EDA community:
EDA tools for logic-logic stacking starting to be developed for um-scale TSVs.
Make sure your algorithms are scalable to nm-scale TSVs… they might happen someday!!