## Slide 1: The Monolithic 3D-IC
A Disruptor to the Semiconductor Industry

## Slide 2: Interconnects Dominate with Scaling [Source: ITRS]
MonolithIC 3D Inc. Patents Pending
2
Transistors keep improving
Surface scattering, grain boundary scattering and diffusion barrier degrade RC delay
Low k helps, but not enough to change trend
 | 90nm (2005) | 45nm (2010) | 22nm (2015) | 12nm (2020)
Transistor Delay | 1.6ps | 0.8ps | 0.4ps | 0.2ps
Delay of 1mm long Interconnect | 5x102ps | 2x103 ps | 1x104 ps | 6x104 ps
Ratio | 3x102 | 3x103 | 4x104 | 3x105

## Slide 3: Interconnect delay a big issue with scaling
MonolithIC 3D Inc. Patents Pending
3
Transistors improve with scaling, interconnects do not
Even with repeaters, 1mm wire delay ~50x gate delay at 22nm node
Source: ITRS

## Slide 4: The Solution - 3D IC
1950s
Too many interconnects to manually solder  interconnect problem
Solution: The (2D) integrated circuit
Kilby version:
Connections not integrated
Noyce version (the monolithic idea):
Connections integrated
Today
Interconnects dominate performance and power and diminish scaling advantages  interconnect problem
Solution: The 3D integrated circuit
3D with TSV: TSV-3D IC
Connections not integrated
Monolithic 3D: Nu-3D IC
Connections integrated

## Slide 5: Monolithic 10,000 x Vertical Connectivity vs. TSV
TSV size typically ~5um:
Limited by alignment accuracy and silicon thickness
Processed Top Wafer
Processed Bottom Wafer
Align and bond
 | TSV | Monolithic
Layer Thickness | ~50m | ~50nm
Via Diameter | ~5m | ~50nm
Via Pitch | ~10m | ~100nm
Wafer (Die) to Wafer Alignment | ~1m | Alignment => Will keep scaling

## Slide 6: The Monolithic 3D Challenge
MonolithIC 3D Inc. Patents Pending
6
A process on top of copper interconnect should not exceed 400oC
    How to bring mono-crystallized silicon on top at less than 400oC
    How to fabricate advanced transistors below 400oC
Misalignment of pre-processed wafer to wafer bonding step is ~1m
    How to achieve 100nm or better connection pitch
    How to fabricate thin enough layer for inter-layer vias of ~50nm

## Slide 7: Path 1 - RCAT
MonolithIC 3D Inc. Patents Pending
7
A process on top of copper interconnect should not exceed 400oC
    How to bring mono-crystallized silicon on top at less than 400oC
    How to fabricate advanced transistors below 400oC

## Slide 8
MonolithIC 3D Inc. Patents Pending
8
step 1 - Implant and activate unpatterned N+ and P- layer regions in standard donor wafer at high temp. (~900oC) before layer transfer. Oxidize top surface (CVD)
Step 1. Donor Layer Processing
step 2 - Implant H+ to form cleave plane for the ion cut
N+
P
-
P-
-
N+
P
-
P-
H+ Implant Cleave Line in N+ or below
SiO2 Oxide layer (~100nm) for oxide –to-oxide bonding with device wafer: planarize with CMP or plasma.
Notes: 8
8

## Slide 9
MonolithIC 3D Inc. Patents Pending
9
step 3 - Bond and Cleave: Flip Donor Wafer and Bond to Processed Device Wafer
Processed Base IC
Cleave along
H+ implant line using 400oC anneal or sideways mechanical force.
Polish with CMP.
-
N+
P-
Silicon
SiO2 bond layers on base and donor wafers (alignment not an issue with blanket wafers)
<200nm)
Notes: 9
9

## Slide 10
MonolithIC 3D Inc. Patents Pending
10
step 4 - Etch and Form Isolation and RCAT Gate
+N
P-
Processed Base IC
Gate
Oxide
Isolation
Litho patterning with features aligned to bottom layer.
Etch shallow trench isolation (STI) and gate structures
Deposit SiO2 in STI
Grow gate with ALD, etc. at low temp
(<350º C oxide or high-K metal gate)
Ox
Ox
Gate
Advantage: Thinned donor wafer is transparent to litho, enabling direct alignment to device wafer alignment marks: no indirect alignment.
Notes: 10
10

## Slide 11
MonolithIC 3D Inc. Patents Pending
11
step 5 – Etch Contacts/Vias to Contact the RCAT
+N
P-
Processed Base IC
Complete transistors, interconnect wires on ‘donor’ wafer layers
Etch and fill connecting contacts and vias from top layer aligned to bottom layer
Notes: 11
11

## Slide 12: Path 2 – Leveraging Gate Last + Innovative Alignment
MonolithIC 3D Inc. Patents Pending
12
Misalignment of pre-processed wafer to wafer bonding step is ~1m
    How to achieve 100nm or better connection pitch
    How to fabricate thin enough layer for inter-layer vias of ~50nm

## Slide 13
Fully constructed transistors attached to each other; no blanket films.
proprietary methods align top layer atop bottom layer
Device wafer
Donor wafer
A Gate-Last Process for Cleave and Layer Transfer
NMOS
PMOS
Poly
Oxide
Notes: 13

## Slide 14
Step 3.
Implant H for cleaving
Step 4.
Bond to temporary carrier wafer
(adhesive or oxide-to-oxide)
Cleave along cut line
CMP to STI
H+ Implant Cleave Line
Carrier
STI
A Gate-Last Process for Cleave and Layer Transfer
CMP to STI
Notes: 14

## Slide 15
Step 5.
Low-temp oxide deposition
Bond to bottom layer
Remove carrier
Step 6. On transferred layer:
Etch dummy gates
Deposit gate dielectric and electrode
CMP
Etch tier-to-tier vias thru STI
Fabricate BEOL interconnect
A Gate-Last Process for Cleave and Layer Transfer
Carrier
Oxide-oxide bond
Remove (etch) dummy gates, replace with HKMG
Notes: 15

## Slide 16: Novel Alignment Scheme using Repeating Layouts
Even if misalignment occurs during bonding  repeating layouts allow correct connections.
Above representation simplistic (high area penalty).
Bottom layer
layout
Top layer
layout
Landing pad
Through-layer connection
Oxide
Notes: 16

## Slide 17: A More Sophisticated Alignment Scheme
Bottom layer
layout
Top layer
layout
Landing pad
Through-layer connection
Oxide
Notes: 17

## Slide 18: Scaling with 3D or Conventional 0.7x Scaling?
3D can give you similar benefits vis-à-vis a generation of scaling!
Analysis with 3DSim Same blocked scaled | 2D-IC @22nm | 2D-IC @ 15nm | 3D-IC 2 Device Tiers @ 22nm
Frequency | 600MHz | 600MHz | 600MHz
Metal Levels | 10 | 12 | 10
Die Size (Active silicon area) | 50mm2 | 25mm2 | 24mm2
Average Wire Length | 6um | 4.2um | 3.1um
Av. Gate Size | 6 W/L | 4 W/L | 3 W/L
Power | 1.6W | 0.7W | 0.8W
Notes: 18

## Slide 19
Courtesy: GlobalFoundries
Notes: 19

## Slide 20: Severe Reduction in Number of Fabs
(Source: IHS iSuppli)

## Slide 21: The Next Generation Dilemma: Going Up or Going Down?
Scale Down 0.7x
Scale Up 2D 3D
Cost: Capital > $4B
R&D Cost > $1B
Benefits: Logic Die Size  0.5x
Power  0.5x
for Speed  No Change
Cost: Capital < $100M
R&D Cost < $100M
Benefits: Logic Die Size  0.5x
Power  0.5x
for Speed  No Change
Monolithic 3D
x0.7 Scaling
Notes: 21

## Slide 22: Summary
Monolithic 3D is possible and practical
Monolithic 3D provides the equivalence of one process node for each folding
  Older Fabs can re-invent themselves and compete with leading edge
  Leading edge fabs could add significant value

## Slide 23: Backup: 3D CMOS Approach:
MonolithIC 3D Inc. Patents Pending
23
p- Si
Silicon dioxide
n+
n+
Gate electrode
Build transistor layers above wiring layers monolithically @ <400oC
Requires novel transistors for logic:
Recessed channel transistors.
Sub-400oC stacking possible.
Used in DRAM and TFT applications today.
nMOS and pMOS recessed channel devices on the same wafer
nMOS and pMOS recessed channel devices on stacked wafers
Notes: 23
23